| Should be used |
| --- |
|  | • Rotary screw compressors for cooling lubricants • Recommended in the outlet temperature> 90 ℃, and / or export> 10bars use |

| Characteristics |
| --- |
|  | • You can optimize the efficiency of the compressor • Good oil / gas and oil / condensate separation performance • protection against wear or corrosion screw • compressed air can really reduce the operating costs • Use the most efficient compressor • increase oil change intervals, drain intervals may be fixed compressors generally use 4000 ~ 6000 hours • If lubrication monitoring, up to 8000 hours • You can extend the life of the separator filter unit • Excellent anti-clogging performance, using a filter with an extended period (up to 8000 hours) |

| Technical Specifications |
| --- |
|  | Typical data Unit Test method DACNIS SH 32 46 68 100 Density (15 ℃) kg/m3 ASTM D1298 859 862 840 869 Viscosity (40 ℃) mm2/s ASTM D445 32 46 68 100 Viscosity Index - ASTM D2270 136 139 147 143 Pour Point ℃ ℃ ASTM D97 <-42 <-42 <-42 <-39 Flash point (open cup) ℃ ASTM D92 250 255 262 265 Specification NF-ISO 6743 classified DAJ areas for heavy |